Technical Data Sheet

ALPHAFLOC

Formulation for flocculation of fine particulates in Colour baths

COMPOSITION AND APPLICATION

Alphafloc is an flocculating additive for colour baths where fine particulates need to be removed. The Alphafloc causes the fine particles to floc together into larger masses that can be more easily filtered out.

PREPARATION AND WORKING CONDITIONS

The dosage rate is maximum 500 mls. per 1000  Ltr.  for the initial clean up dose.

Do some initial lab test to establish what dosage is required. Use as little as required to do the job.

You can eliminate the precipitate from the electrolyte, with either filtration, allowing it to settle, or a combination of both.

The use of this floc in the initial dose, also seems to reduce the soluble tin by about 10%.

Continue doing a weekly dose of about 5-10% of the initial dose ( 250-500 mls. per 10000 ltr)

Again use the minimum amount required to achieve a clear solution.

The main benefit of the clear electrolyte solution is clean work at the end of the line.

In individual cases the optimal operating parameters may vary from the given standard parameters.

Safety Precautions:

Please observe the usual safety precautions for handling chemical substances. Classifications according to the statutory regulations for transport, storage and handling of the product and other product-specific instructions are included in the SDSt. Bath solutions, rinse water and concentrates must be treated according to the applicable regulations before entering the sewage system.